The following specification has been developed by

Marlite

202 Harger St.

Dover, Ohio 44622

Tel: (330) 343-6621 Fax: (330) 343-4668.

Email:  info@marlite.com  www.marlite.com

to assist Architects and Designers in the specification of Decorative Fiberglass Reinforced Plastic wall panel system for high wear areas.

Marlite Stamdard FRP Panels are excellent for sanitary environments since they facilitate washing and cleaning and do not support mold or mildew growth.  However, FRP panels are subject to the effects of continuous humidity and temperature.  Provide adequate ventilation for drying and do not use in high temperature areas.

Marlite Induro FRP provides an exceptionally wear resistant decorative panel; due to an exclusive process of thermally bonding melamine impregnated surfacing materials directly to the FRP core.  Designed to match or coordinate with popular High Pressure Laminates, these panels offer a superb array of decorative finishes and patterns from solid colors to wood-grains and abstract patterns.  Custom color and patterns are available upon request.

Marlite Artizan FRP panels offer a superb array of decorative printed rotogravure finishes with exceptional image integrity; unlimited varieties of woodgrain and abstract pattern plus tactile as well as visual textures.  Custom color and patterns are available upon request.

Marlite Envue Graphic FRP provides impressive visuals of high-resolution photographs, illustrations, logos, tile designs and custom graphics, all protected by Marlite’s tough Sani-Coat sealer. A special application process produces optimum graphic reproduction on a tough, sanitary surface.

Marlite Symmetrix with Sani-Coat FRP panels feature prefinished precision grid score lines that provide the look of tile without grout to clean or deteriorate.  Custom color and patterns are available upon request.

The section has been formatted in accordance with the principals embodied in the Construction Specifications  Institute's  Manual of Practice and is intended for use in conjunction with Contract Conditions, Bidding Conditions and General Requirements developed in accordance with CSI guidelines.

Notes to the specifier are included. Options that must be selected by the specifier are shown in brackets [         ].   Inapplicable clauses shall be deleted.

SECTION 09 7720 – FIBERSCORE FIBERGLASS REINFORCED WALL PANELS

GENERAL

SUMMARY

Section Includes:  Prefinished polyester glass reinforced plastic sheets and adhered to unfinished [gypsum] [cementitous] [untreated plywood] wallboard.

[Aluminum] [PVC] trim.

[PVC Wall base.]

Products Not Furnished or Installed under This Section:

Gypsum [Cementitious] substrate board.

Resilient Base.

RELATED SECTIONS

Section [____] – 	Gypsum [Cementitious] substrate board.

Section [____] - Wood [Metal] Stud Framing

Section [____] - Painting & Transparent Finishes.

Section [____] - Resilient Base.

REFERENCES

References are listed as a convenience and are often deleted in their entirety.  If required by the user agency delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials:  Standard Specifications (ASTM)

ASTM D 256 -	Izod Impact Strengths (ft #/in)

ASTM D 570 -	Water Absorption (%)

ASTM D 638 -	Tensile Strengths (psi) & Tensile Modulus (psi)

ASTM D 790 -	Flexural Strengths (psi) & Flexural Modulus (psi)

ASTM D 2583- Barcol Hardness

ASTM D 5319 - Standard Specification for Glass-Fiber Reinforced Polyester Wall and Ceiling Panels.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

SUBMITTALS

Product Data:  Submit sufficient manufacturer's data to indicate compliance with these specifications, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings:  Submit elevations of each wall showing location of paneling and trim members with respect to all discontinuities in the wall elevation.

Selection Samples:  Submit manufacturer’s standard color pattern selection samples representing manufacturer's full range of available colors and patterns.

Samples for Verification:   Submit appropriate section of panel for each finish selected indicating the color, texture, and pattern required.

Submit complete with specified applied finish.

For selected patterns show complete pattern repeat.

Exposed Molding and Trim:  Provide samples of each type, finish, and color.

Manufacturers Material Safety Data Sheets (MSDS) for adhesives, sealants and other pertinent materials prior to their delivery to the site (available as downloads for most Nudo’s products at http://nudo.com/literature.php or by contacting Nudo at info@nudo.com).

QUALITY ASSURANCE

Conform to building code requirements for interior finish for smoke and flame spread requirements as tested in accordance with:

ASTM E 84 (Method of test for surface burning characteristics of building Materials)

Wall Required Rating – Class [C].

Include the following if products are used in areas subject to stringent wash down requirements.

### Sanitary Standards:  System components and finishes to comply with:

United States Department of Agriculture (USDA) requirements for food preparation facilities, incidental contact.

#### Food and Drug Administration (FDA) 1999 Food Code 6-101.11.

Canadian Food Inspection Agency (CFIA) requirements.

DELIVERY, STORAGE AND HANDLING

Deliver materials factory packaged on strong pallets.

Store panels and trim lying flat, under cover and protected from the elements.  Allow panels to acclimate to room temperature (70°) for 48 hours prior to installation.

PROJECT CONDITIONS

Environmental Limitations:  Building are to be fully enclosed prior to installation with sufficient heat (range of 60° to 75°) and ventilation consistent with good working conditions for finish work

During installation and for not less than 48 hours before, maintain an ambient temperature and relative humidity within limits required by type of adhesive used and recommendation of adhesive manufacturer.

Provide ventilation to disperse fumes during application of adhesive as recommended by the adhesive manufacturer.

WARRANTY

Furnish one year guarantee against defects in material and workmanship.

PRODUCTS

ACCEPTABLE MANUFACTURER

Nudo; 1500 Taylor Avenue, Springfield, IL 62703.  (217) 528-8722 FAX (217) 528-5636 Email:  info@nudo.com http://www.nudo.com/.

Product:

FiberScore FRP with Sani-Coat

PANELS

Fiberglass reinforced thermosetting polyester resin panel sheets complying with ASTM D 5319.

Coating:  Multi-layer print, primer and finish coats or applied over-layer.

Dimensions:

Thickness – 0.090 “ (2.29mm) nominal

Width - 4'-0”  (1.22m) nominal

Induro FRP Panels are not available in lengths exceeding 8’ (2.4m).

Length – [10’-0” (3.0m)][8’-0” (2.4m) ][As indicated on the drawings] nominal

Tolerance:

Length and Width:  +/-1/8 “ (3.175mm)

Square -  Not to exceed 1/8 “ for 8 foot (2.4m) panels or 5/32 “ (3.96mm) for 10 foot (2.4m) panels

Properties:  Resistant to rot, corrosion, staining, denting, peeling, and splintering.

Flexural Strength - 1.0 x 104 psi per ASTM D 790. (7.0 kilogram-force/square millimeter)

Flexural Modulus - 3.1 x 105 psi per ASTM D 790. (217.9 kilogram-force/square millimeter)

Tensile Strength - 7.0 x 103 psi per ASTM D 638. (4.9 kilogram-force/square millimeter)

Tensile Modulus - 1.6 x 105 psi per ASTM D 638. (112.5 kilogram-force/square millimeter)

Water Absorption - 0.72% per ASTM D 570.

Barcol Hardness (scratch resistance) of 35 55 as per ASTM D 2583.

Izod Impact Strength of 72 ft. lbs./in ASTM D 256

Back Surface:  Smooth. Imperfections which do not affect functional properties are not cause for rejection.

Select finish from our full Marlite Finish Palette at www.marlite.com or contact Marlite to create your own finish.

Front Finish: [As Indicated on the Drawings] [In accordance with preapproved sample.  Information available from the Architect’s Office][ __________________________________}

        - Color: [Specifier to choose.]

FiberScore FRP with Sani-Coat FRP is available in the following colors:

50-G44 White

        - Fire Rating FiberScore FRP is available in Class C (III) Fire Rating.

        - Size: [Specifier to choose, or as indicated on drawings.] standard sizes are;

          - FiberScore FRP

            - 48” x 96” [1.2m x 2.4m] x .090” (3mm) nom.

            - 48” x 120” [1.2m x 3m] x .090” (3mm) nom.

ACCESSORIES

Fasteners: Provide appropriate fasteners and accessories as required to properly complete installation

Adhesive: Provide panel adhesive as recommended by panel manufacturer.

Trim and Seam Treatment:

Manufacturer: Acceptable to panel manufacturer.

Manufacturer Designation: [Corner molding] [Division bar] [Cap] [Specify manufacturer designation.].
Specifier Note: Retain one of three subparagraphs below to suit project requirements.

Material and Color: Color matched acrylic latex caulk.

Material and Color: [Aluminum moldings ] [Specify color ]

Material and Color: [Standard PVC Moldings ] [Specify color ]

Select PVC or Aluminum trims.

EXECUTION

PREPARATION

Examine backup surfaces to determine that corners are plumb and straight, surfaces are smooth, uniform, clean and free from foreign matter, nails countersunk, joints and cracks filled flush and smooth with the adjoining surface.

Verify that stud spacing does not exceed 24” (61cm) on-center.

Repair defects prior to installation.

Level wall surfaces to panel manufacturer’s requirements.  Remove protrusions and fill indentations.

INSTALLATION

Comply with manufacturer's recommended procedures and installation sequence.

Cut sheets to meet supports allowing 1/8” (3 mm) clearance for every 8 foot (2.4m) of panel.

Cut and drill with carbide tipped saw blades or drill bits, or cut with shears.

Pre-drill fastener holes 1/8” (3mm) oversize with high speed drill bit.

Space at 8” (200mm) maximum on center at perimeter, approximately 1” from panel edge.

Space at in field in rows 16’ (40.64cm) on center, with fasteners spaced at 12” (30.48 cm) maximum on center.

Apply panels to board substrate, above base, vertically oriented with seams plumb and pattern aligned with adjoining panels.

Install panels with manufacturer's recommended gap for panel field and corner joints.

Adhesive trowel and application method to conform to adhesive manufacturer’s recommendations.

Drive fasteners for snug fit.  Do not over-tighten.

Apply panel moldings to all panel edges using silicone sealant providing for required clearances.

All moldings must provide for a minimum 1/8 “ (3mm) of panel expansion at joints and edges, to insure proper installation.

Apply sealant to all moldings, channels and joints between the system and different materials to assure watertight installation.

CLEANING

Remove excess sealant from panels and moldings.  Wipe panel down using a damp cloth and mild soap solution or cleaner.

Refer to manufacturer's specific cleaning recommendations Do not use abrasive cleaners.

END OF SECTION 09 7720